## Slide 1: Thermal Runaway & TFPX
Jim Alexander
weekly TFPX Mechanics mtg
16 April 2019

## Slide 2
Part I:
Dark Currents in depleted silicon devices

## Slide 3: Temp dependence of dark current
We don’t know the constant, but can “calibrate”:

 Heat generated in silicon grows exponentially with temp

## Slide 4: Temp dependence (cont’d)
Clarify “Heat generated in silicon grows exponentially with temp”
TA ≃ Eg/2kB
where Eg ≃ silicon band gap = 1.12 eV (but increases with damage)
kB = Boltzman’s const
So TA ≃ 7000K >> T, Tref  approximations are handy

T1/2 ≃ 6.5 oC doubling temp
some algebra…
depends on Eg, Tref!!
I use Eg=1.2 eV throughout
handy for mental calculations but I use the real formula throughout this doc

## Slide 5: Radiation Damage
Expected Fluence for TFPX
  based on FLUKA studies, innermost edge of our ring-1 sensors will see about 2x1016 neq/cm2 by end of HL-LHC.
  Allowing for uncertainties in FLUKA (30% according to the TDR) and uncertainty in ultimate integrated luminosity (maybe 4000/fb in some plans/dreams) we need to plan for about 3x1016. [These numbers need to be firmed up.]
Silicon detector dark current grows linearly with fluence
  heavy particle (n,p) collisions with Si nuclei damage the crystal lattice, creating new quantum levels between valence and conduction band
  Michael Moll’s PhD thesis is the bible of this field

## Slide 6: Dark Current density vs Fluence
Layer 1
Layer 2
Layer 3
Layer 4
Michael Moll
PhD thesis
slope=4.28x10-17 A/cm
uncertainty in sensor temp
included in size of red dot
current at 20 degC
ATLAS pixel
CMS Phase 1 BPIX
B-layer
Layer-1
Layer-2
CMS BPIX source: Finn Feindt, indico=769192, Feb 2019
ATLAS Source: S. Seidel, indico=777112, Feb 2019
Note: ATLAS data need clarification)
3E16
1.3A/cm3
data are scaled to currents at +20 oC

## Slide 7: Consequences: I x V = power
1.3A/cm3 @20C translates to 1.6mA in a 1x2 module operating at -20C.
At the anticipated 800V operating bias, the sensors in a 1x2 module will generate 1.3 W.
Summary: For 1x2 sensor @…
Fluence = 3e16
Sensor temp = -20C
Depletion depth = 100um
Vbias = 800
heat output = Q = 1.3W
sensor volume
Fluence

## Slide 8: Exponential Heat Load (Q vs T)
Tref = 0 oC
Qref = 2,4,8 W
8 W
4 W
2 w
direction of radiation damage
Q
T

## Slide 9: Cooling is a linear process
T0=-20C
worse cooling (higher R)
Q
Rth
T0
T
Stable Operating Point
better cooling
(lower R)

## Slide 10: Cooling a nonlinear system…
Unstable Equilib
No equilibrium at all—
total runaway…
disaster.
For a given heat load Q, there is a minimum thermal resistance R needed to maintain a stable temp.
In both cases, Rth is too high:
bad design / bad implementation
Note: T0 is same in both cases: this will be our situation since T0=-33C is fixed already by cooling experts.

## Slide 11
Part II:
Runaway calcs & estimates in T(B/F)PX

## Slide 12: Some numbers from TBPX
Use Perugia thermal studies to estimate their total R from heat source (ROC) to sink (CO2), indico 770283
Q=2x2.06+0.6W
Q=2.43W
Q=2.91W
DT ≃ |33-20|=13oC
DT ≃ |33-18|=15oC
DT ≃ |33-16|=17oC
 R ≃ 13/2.06=2.8oC/W
 R ≃ 15/2.43=2.8oC/W
 R ≃ 17/2.91=2.7oC/W
Conclusion: Reff ~ 3 oC/W

## Slide 13: More on TBPX numbers…
Replace ANSYS with a simple model that focusses on key design parameters
Reff ~ 3 C/W
T0
T
ROC
ROC
HDI
2.43W nom.
2.43W nom.
0.57W nom.
R ~ 0
CO2 Temp == -33 oC
inferred effective thermal resistance, Reff
sensor temp
Sensor
Q(T)
R ~ 0

## Slide 14: How far is TBPX from runaway?
R=2.15 oC/W
Bianchi
indico 770283
Francesco is asking: “If the CO2 temp changes by X, when do we hit runaway?”
His answer: X=5oC.
5oC
5oC
Tsens=TCO2 + 15oC
Tsens=TCO2 + 15oC
Baseline heat load due to ROCS and HDI = 5.43 W
Fluence 2.1E16
0.109cm3 sens volume
600V bias

## Slide 15: How far is TBPX from runaway?
But this is the wrong question. He is asking “if we get into trouble, by how much do we have to turn down the CO2 temperature?”
The right question is: “What value of R do we have to design to to ensure adequate margin of safety against runaway?”
R=2.15 C/W in current TBPX design
R*=2.15x1.25 C/W puts you in runaway
25% worse R
(for fixed TCO2)
TCO2 is already fixed and outside our control
TCO2=-33
Fluence 2.1E16
0.109cm3 sens volume
600V bias

## Slide 16: Bottom-up estimate of TBPX Reff
use dimensions the k-values taken from TBPX slides
Silicon (sensor)
Silicon (ROC)
Alum-Nitride
Carbon Fiber
Alum-CarbFib
SS pipe
CO2
bilateral symmetry
TBPX simplified model
adhesives etc are included but not shown in this diagram

## Slide 17: Bottom-up Estimate: Numbers
Use dimensions the k-values taken from TBPX slides to compute approximate effective thermal resistance, Reff in this crude model:
Result (oC/W)
Bottom-up model gives Reff in right ballpark but a bit high.
(could fine-tune inputs, but…)
May be reliable, however, in identifying main culprits.

## Slide 18: TFPX geometry is a bit different
At least in the context of these highly simplified models, it looks like TFPX geometry offers more parallelism in thermal paths
TFPX simplified model
Silicon (sensor)
Silicon (ROC)
adhesive/alternative
Carbon Fiber
Carbon Foam
epoxy
SS pipe
CO2
Result (oC/W)

## Slide 19: Implications of Reff = 1.5oC/W
Thermal performance of TFPX estimated from the crude model of previous slide
1.8 x R
Fluence 2.1E16
0.109cm3 sens volume
600V bias
(to match TBPX calcs)
TCO2 = -33
R=1.5 C/W
Baseline heat load due to ROCS and HDI = 5.43 W
R*=1.75x1.8 C/W puts you in runaway
(for fixed TCO2)

## Slide 20: Consider temp variations over sensor
Perugia temp maps suggest T(x,y) = Tavg +/- 6 oC
Implications for TFPX shown below; still some margin of safety
Tavg
Tavg-6oC
Tavg+6oC
R=1.5 C/W
R= 1.35 * 1.5 C/W
TCO2 = -33

## Slide 21: Include variations in ROC power
Consider also “worst” case for ROC power output  2.91W
Implications for TFPX shown below; still some margin of safety
Tavg
Tavg-6oC
Tavg+6oC
R=1.5 C/W
R= 1.25 * 1.5 C/W
Increase ROC to 2.91W/chip
TCO2 = -33

## Slide 22: Consider ROC failure scenarios
significant increase in heat load if one ROC fails?
details to be filled in….

## Slide 23: Observations
TBPX looks marginal (25% safety factor). This is based on the Reff derived from their ANSYS study.
For TFPX we can crudely estimate Reff by adding up rough values of R for each layer. The same procedure applied to TBPX overestimated R by about x1.5 compared to the ANSYS-implied value… but it’s hard to know how good/bad this crude model is.
For TFPX, the crude model gives R=1.5 C/W.
Applying this to the runaway calculation, we find an 80% safety factor… for uniform sensor temps & nominal ROC power
Including nonuniform temps and worst-case ROC power, margin decreases to 25%. Yet worse cases can and should be explored. Note that Fluence assumed is worst case (inner radius) already.
Simple geometric differences between TBPX and TFPX thermal pathways strongly suggest that TFPX should have lower R than TBPX.
The ANSYS-derived plots that TBPX shows do not seem to be a transparently useful tool for setting design specs. But they can be translated into one.

## Slide 24: Where do we go from here
Continue the experimental studies in G14 to obtain empirical measurements of Reff under various design options
Pair those studies with ongoing ANSYS simulations to develop skills and confidence in this powerful tool
Apply ANSYS to the full dee design (perhaps one module at a time…) with latest parameters from Yadira. (Yadira started training me on this; I’m gonna need helpers.)
Perugia….
At all points in this process, assess safety margin in Reff:
  what are the dominant factors that determine Reff?
  what design modifications are likely to be profitable?
  do experimental tests of those alternatives confirm expectations of improvement? If not, why not?